## Slide 1
Benjamin Gladwyn
Wednesday Group Meeting
07/12/2023
bengladwyn/Fermilab: Measuring the properties of Ferrites for RF cavities (github.com)
Measurements of Energy Losses in Ferrite Samples

## Slide 2: Relative Permittivity and Permeability Measurements
Measure s-parameters of empty holder and when sample is present
Manipulate phases to realize phases of the garnet sample only
Phase of ½ inch sample + fittings
Phase of empty holder and fittings
Calculated phase of ½ inch of air
=

## Slide 3: Relative Permittivity and Permeability Measurements
Measure s-parameters of empty holder and when sample is present
Manipulate phases to realize phases of the garnet sample only
Use the Nicholson-Ross-Weir (NRW) method to calculate and
Phase of ½ inch sample + fittings
Phase of empty holder and fittings
Calculated phase of ½ inch of air
=
Simulation
Measurements
?

## Slide 4: Relative Permittivity and Permeability Measurements
Using these phase manipulations the Nicholson-Ross-Weir Method correctly determines and for the simulations.
It produces the following for measurements taken from the equipment
Sample L74087BAN4
?
Negative

## Slide 5: Relative Permittivity and Permeability Measurements
Across the frequency spectrum at different bias currents we have the following
Sample L74087BAN4
0A
10A
25A

## Slide 6: Loss Measurements
Loss quantified with . Comparison of the samples (one from each batch) on different days we see the same trend, just with a different calibration.
07/10/2023
07/11/2023

## Slide 7: Loss Measurements
07/10/2023 – 2 different samples of each batch measured
07/11/2023 – 3 different samples of each batch measured
No discernible differences between the batches, only between samples.
07/10/2023
07/11/2023